## Slide 1
Radiative/Nonradiative Recombination Mechanism
Nonradiative Recombination in CdTe
Modified SRH Recombination Models for VCd
Conducting
edges
Carrier capture processes in CuIn1-xGaxSe2 and CdSe1-xTex solar cells materials
Xiaofeng Xiang1 and Scott T. Dunham2
1Molecular Engineering & Sciences
2Department of Electrical & Computer Engineering
University of Washington, Seattle, WA, 98195
Deep Level Defects in Cu(In,Ga)Se2
Introduction
Point defects directly impact solar cell device performance by nonradiative recombination and thus limit carrier lifetime and device efficiency.
In this work, density functional theory calculations are used to identify and characterize nonradiative recombination centers and corresponding capture cross sections in CuIn1-xGaxSe2 and CdSe1-xTex solar cell materials.
The calculated defect densities as well as the corresponding capture cross sections and trap energy levels can be implemented into Shockley-Read-Hall (SRH) type recombination models to calculate carrier lifetimes. Modified SRH equations are required for CdSe1-xTex solar cells due to multiple configurations of metastable deep level defects. These models are implemented into device simulation model to predict and optimize solar cell efficiency.
R1:
R2:
R3:
R4:
R5:
R6:
R7:
Chart: VCd Recombination Processes (Injection Level 1e15)
| R1 | R2 | R3 | R4 | R5 | R6 | R7
Ef=0.66 eV | 5958140 | 5957420 | 2.4595e+17 | 89372100000000000 | 64056.1 | 1.5658e+17 | 1.5658e+17
Ef=0.16 eV | 735.875 | 736.862 | 1234170000000000 | 448459000000000 | 321.427 | 785709000000000 | 785709000000000
Ef=0.86 eV | 327.483 | 328.565 | 13518600000000 | 4912240000000 | 3.5208 | 8598520000000 | 8598520000000
Chart: VCd Recombination Processes (Injection Level 1e13)
| R1 | R2 | R3 | R4 | R5 | R6 | R7
Ef=0.66 eV | 747.055 | 897.201 | 30839100000000 | 11206000000000 | 0.080317 | 19633100000000 | 19633100000000
Ef=0.16 eV | 7.3121 | 7.0094 | 1196470000000000 | 434759000000000 | 3.1161 | 761706000000000 | 761706000000000
Ef=0.86 eV | 0.04106 | 0.041071 | 1694990000 | 615907000 | 4.4144e-06 | 1079080000 | 1079080000
CB
VB
Eg
E
According to Fermi’s golden rule
Electron-phonon coupling matrix element
AM1.5 Global
CIGS
Mo
CdS
ZnO
AZO
MgF2
 | JSC (mA) | VOC (V) |  (%) | FF
Experiment [4] | 34.7 | 0.7113 | 19.0 | 77.1
Sentaurus Model | 34.7 | 0.7146 | 19.3 | 77.6
Step (1) change of the electronic state due to electron-phonon coupling (Nonradiative).
Step (1*) change of the electronic state due to electron-photon coupling (Radiative).
Step (2) vibrational relaxation due to phonon-phonon interactions.
Algorithm of Nonradiative/Radiative Recombination [1]
Configuration coordinate diagram (left) and Band diagram (right)
We applied above method to examine possible deep level defects in CuIn1-xGaxSe2, such as antisites (CuIII, GaCu, etc) and complexes (InCu+2VCu, InCu+ CuIII +VCu, etc). We found only CuIII (-1/0) has both large capture coefficient and significant defect concentration in CIGS.
To simplify the problem, only one special phonon mode is used to replace the sum over all vibrational degrees of freedom. Thus,
To implement above theories, Nonrad [2] code is used to calculate and capture coefficients from first principles. However, if large structural distortions appears after carrier capture, we may not see harmonic function in configuration coordinate diagram as shown above. Under such circumstance, another package CarrierCapture.jl [3] is applied to deal with anharmonicity..
Configuration coordinate diagram of CuIn (-1/0) (left) and CuIn(-2/-1) (right)
The capture coefficient/capture cross section obtained from Nonrad is implemented into SRH model in device simulation. We use such model to compare with experiment and find they have close match.
References
Device schematic of CIGS solar cell
Comparison between device simulation and experiment
[1] Alkauskas, Audrius, Qimin Yan, and Chris G. Van de Walle. Physical Review B 90.7 (2014): 075202.
[2] Turiansky, Mark E., et al. Computer Physics Communications 267 (2021): 108056.
[3] Kim, Sunghyun, et al. Journal of Open Source Software 5.47 (2020): 2102.
[4] Jackson, Philip, et al. Progress in Photovoltaics: Research and Applications 15.6 (2007): 507-519.
[5] Kavanagh, Seán R., Aron Walsh, and David O. Scanlon. ACS energy letters 6.4 (2021): 1392-1398.
Next steps: We will keep exploring other possible deep level defects and build coupled materials/process/device models for CdTe1-xSex photovoltaics.
In n-type, p-type, or nearly intrinsic CdTe, . Thus, (-1, 0_dimer) transition is the dominant recombination process.
When injection level is higher than 107 cm-3, R3/R4 becomes a constant value. We can then derive a new SRH model to be implemented into device simulation
A dominant recombination center identified by researchers is VCd. VCd goes through a large structure distortion when the charge state changes from 0 to -2 [5].
Td-symmetry
(a1=a2=a3=a4)
C3v-symmetry
(a1>a2=a3=a4)
C2v-symmetry
(a1=a4≠a2=a3)
Recombination Rate Comparison under Various Conditions
Schematic of the non-radiative recombination mechanism of VCd
This work was supported in part by the U.S. Department of Energy's Office of Energy Efficiency and Renewable Energy (EERE) under the Solar Energy Technology Office Award Number DE-EE0008556. The authors would also like to thanks the Clean Energy Institute (CEI) at the University of Washington for fellowship support (2020-2021). This work was facilitated through the use of the Hyak supercomputer system at the University of Washington supported via the Student Technology Fund.
Defect | σp (cm2) | σn (cm2)
InCu+CuIII+VCu | 1.14E-25 | 1.01E-27
2VCu+InCu | 1.88E-25 | 1.66E-27
CuIII | 7.41E-13 | 2.47E-16
GaCu | 1.34E-24 | 3.68E-21
Table of defect capture cross sections in CuIn1-xGaxSe2
a1
a2
a3
a4
a1
a2
a3
a4
a2
a1
a3
a4
Te
Te
Te
In principle, radiative and non-radiative processes are competing. Radiative rate are of the order 10-14 - 10-13 cm3 s-1. Nonradiative rate are over range of 10-14 - 10-6 cm3 s-1. In both processes, step (1) is the rate limiting step.
UW Nanotechnology
Modeling Lab